## Slide 1: Variation of SBE (Spent Bleaching earth) Deoiling Treatment’s Effect on Post-Treated SBE (PSBE)’s Quality and Strength Activity Index (SAI)
By: Jordan, Jevon 2023
Quantity
Post Treatment -> Post De-oiled SBE => Treatment => PSBE
Observed from samples containing PSBE; Compared with PCC & Fly ash

## Slide 2: Hypothesis
1. The largest amount of acetone would produce the least amount of oil
2. Fly ash would increase both paste and mortar compressive strength while PSBE would lower both paste and mortar compressive strength
3. PSBE would contain undesirable effect that could affect paste and mortars.

## Slide 3: Testing Guide
Why => Time Constraint, Budget, & Usage
ASCM C1709
Components | Percentage |  | Total (% Al2O3+SiO2+Fe2O3) |  | Total (% SO3) | 
 | PSBE_T | Fly ash | PSBE_T | Fly ash | PSBE_T | Fly ash
Al2O3 | 4 | 7.4 | 68.7 | 64.85 | 1.4 | 2.2
SiO2 | 38 | 20.5 |  |  |  | 
Fe2O3 | 26.7 | 36.95 |  |  |  | 
SO3 | 1.4 | 2.2 |  |  |  | 
ASTM C618
!Doesn’t Guarantee Anything Except the Sole Amount of QTY

## Slide 4: Research Procedure

## Slide 5: Imagery
A
B
C
Deoilling/Treatment Procedure
Paste Making + Testing
Mortar Making + Testing

## Slide 6: 1. Oil Content
This would be chosen as PSBE_T
!No significance difference is found from treating SBE with different quantity
Rp. 450.000,-
Rp. 900.000,-

## Slide 7: 2. Normal Consistency
**Raises the amount of water needed
SEM @1000x
Those with rounder shape would yield a better result since the overall surface area would be larger than those with rough edges or uneven shape (A.M. Neville and J.J. Brooks, Concrete Technology, 2017)
PSBE
Fly ash
**Lowers the amount of water needed
WHY???
Physical Characteristic of The Material

## Slide 8
Water sips in here
Chemical Characteristic of The Material
PBSE_2_5 | 5 | 10 | 30 | 22.86 | 1.1977 | 94.76
PSBE Oil (%)
SBE Oil (%)
! Both Oil & Illite would cause this devastating effect

## Slide 9: 3. Setting Time
! Both PSBE_T & Fly ash Increased Setting Time

## Slide 10
PSBE
Illite, Cristabolite, Sodalite, Gaylusite
Fly ash
Pozzolanic (Tobermorite Gel)
*Found in the metamorphosed lime
PSBE
SBE
Would caused prolonged setting time since the whole thing is wrap
In a gel like substances.
Cristobalite low | SiO2 | 3.04 | 0.19
Illite | Al4KO12Si2 | 15.07 | 8.74
! This Substances Increases
! Both PSBE & Fly ash caused prolonged setting time with different reasons

## Slide 11: 4. Specific Weight
Sample Name | Specific Weight (g/cm3)
PCC | 3
PSBE_T | 2.04
Fly ash | 2.8
Confirmation:
(Changyong et al., 2020)
Nama Sampel | Apparent density (kg/m3)
Cement (PCC) | 3,090
Fly ash | 2,340
PSBE => 1.9-2.1 g/cc (Yulikasari et al., 2021)
! Potential to be used as pavement, light concrete, etc. exists

## Slide 12: 5. Passing Sieve Analysis
Sample Name | Avg. Retained Weight (gr) | Avg. Pass Sieve (gr) | Avg. Total Weight (gr) | Avg. Retained (FM) (%) | Status
PCC | 13.2 | 86.8 | 100 | 13.2 | Pass
Fly ash | 4.33 | 95.67 | 100 | 4.33 | Pass
PSBE_T | 13.73 | 86.2 | 99.93 | 13.74 | Pass
SEM @ 1000x

## Slide 13: 6. Paste Compression Strength
! Addition of substituent materials would lower paste compression
Fly ash > PSBE > SBE
Sodalite | Na8Al6Si6O24BF42 | 12.2 | 3.7
!Sodalite increases material’s strength & Durability (K.M. Klima et al.,2022)
PSBE
SBE

## Slide 14
Designation | PCC | PSBE_T_5 | Flyash_15
OPC | 28.13 | 26.53 | 23.4
S | N.A | N.A | N.A
Total | 28.13 | 26.53 | 23.4
XRD Paste Testing Result
PCC > PSBE_T_5 > Flyash_15
! Slight Warning: I am not a certified chemist nor I ‘d like to be one

## Slide 15: 7. Mortar Flow
Illite
Cristobalite
Increases water demand
Increases viscosity
Gaylussite | Na2Ca (CO3)2H2)5 | 3.09 | 0.72
! Although Gaylusite could improve mortar’s workability,
The amount is relatively small compared with Illite & Cristabolite low

## Slide 16: 7. Hydration Temperature
! Each mortars’ starts in a different starting temperature
PCC has the highest heat gain followed by Fly ash.
! PSBE came in last

## Slide 17
**All four groups contributes to heat generation
Sample Name | Max. Heat Gain (Co) | Phase QTY
PCC | 6.7 | 29.8
PSBE_T_5 | 4.33 | 28.27
! PSBE_T does indeed produce lower heat gain since it has less amount of heat generation substances
Suitable for bricks or pottery

## Slide 18: 8. Mortar Compression Strength
Fly ash > PCC > PSBE > SBE
!This shows the importance of treating SBE before actual usage

## Slide 19
Pozzolanic Reaction is Observed to be active in either concrete or mortar. It is observed that fly ash “competes” with cement in paste samples (Naganathan & Linda, 2013).
! Larger replacement quantity would lead to greater decrease of both mortar and paste compressive strength

## Slide 20: Conclusion
1. Acetone Ratio Doesn’t Have Any Clear Correlation with PSBE Oil Content
2. It is found that there’s four elements that increases after SBE is treated (chem not primary):
3. PSBE decreases both paste and mortar strength. However, using PSBE is better than not treating SBE at all.
Illite => Causes water disruption (Consistency and stuffs)
Sodalite => Increases Material Strength & Durability
Cristobalite => Causes Instability (due to the phase changing); Decreases strength
Gaylusite => Slight Improvement of Workability (but the amount is relatively small)

## Slide 21: Thank You
谢谢大家 